EMG Graphic Systems, Inc. Thermoformed ADA Signage

SPECIFICATIONS

SECTION 10440

INTERIOR SIGNAGE – THERMOFORMED ADA ROOM SIGNAGE

- GENERAL

  - SECTION INCLUDES

    - Interior signage of the following types:

      - Custom thermoformed ADA Room Signage.

  - RELATED SECTIONS

    - Section 10410 - Building Directory.

    - Section 10420 - Dedication Plaque.

    - Section 10430 - Exterior Signage.

  - REFERENCES

    - ICC/ANSI A117.1 - Accessible and Useable Buildings and Facilities.

    - USATBCB - Americans with Disabilities Act (ADA), Accessibility Guidelines for Buildings and Facilities (ADAAG).

  - SUBMITTALS

    - Submit under provisions of Section (TBD).

    - Product Data:  Manufacturer's marketing collateral and specification sheets.

    - Shop Drawings: Include dimensions, colors, thicknesses, and fabrication techniques for each sign type.

    - Samples: One sample of thermoformed plaque to ensure proper fabrication methods.

  - QUALITY ASSURANCE

    - Regulatory Requirements:  Comply with requirements of ICC/ANSI A117.1 and ADAAG.

  - DELIVERY, STORAGE, AND HANDLING

    - Inspect products upon receipt. Store products in manufacturer's packaging until ready for installation.

  - PROJECT CONDITIONS

    - Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.

- PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer:  EMG Graphic Systems, Inc. 1110 North Iroquois Avenue, Tulsa, OK 74106-5901 (918) 835-5300 voice (866) 295-4383 fax

    - Substitutions:  Not permitted.

    - Requests for substitutions will be considered in union with provisions of Section 01600 or on suppliers own form prior to deadline.

  - SIGNS

    - ADA-Compliant Interior Signage, Custom Design.

  - INTERIOR SIGNAGE SCHEDULE

    - Manufacturer’s standard one-piece tactile plaque manufactured utilizing a thermoforming process, which provides a fully integral plaque sign.

- Style.  Thermoformed ADA Signage, Custom Design.

- Material.  Clear Acrylic, Extruded.

- Alternate Materials: Recycled Acrylic Substrate (EcoStrate)

- Thickness.  See drawings for material thicknesses, specified by architect. (Metric millimeter measurements preferred)

- Tactile Characters.  Thermoformed, integral raised copy and braille with spherical dots, raised 1mm (1/32") from sign face.

- Construction. One-piece, thermoformed construction.

- Lettering Style.  Typeface as selected from manufacturer's font collection.  Sans-serif, minumum height 0.625", maximum height 2".

- Braille.  Grade 2 Contracted Braille, placed below last line of copy.

- Color Contrast.  Letters, numbers, and symbols must contrast with the background color.  All raised copy or symbols tip-screened in contrasting color chosen from manufacturer's available color lines.

- Background Color.  Chosen from manufacturer's available color lines, first or second surface.

- Surface Texture. Matte.

- EXECUTION

  - EXAMINATION

    - Examine installation areas to ensure that conditions are suitable for installation.  All walls must have final wall covering or painted finish.  Plaques can not be painted around or removed for painting without damaging plaques.

    - Prior to shipment or installation, plaques are to be checked for defects.

  - PREPARATION

    - Inspect and verify that locations for interior signage will comply with ADA standards.

    - Clean and prepare mounting locations to ensure proper adhesion of double sided foam tape and construction adhesive.

  - INSTALLATION

    - Install signs level and plumb, taking into consideration adjacent features (door frames, wall sconces, etc.) that might affect appearance.

      - Mount with vinyl foam tape and construction adhesive or silicone adhesive.

      - Mount with screws through exposed sign face.

      - Mount first surface painted plaques with 1/8" diameter spring pins when size or wall covering dictates.

    - Clean signs after installation as recommended by manufacturer.

    - Replace damaged signage, if any, before Substantial Completion.

  - INTERIOR SIGNAGE SCHEDULE

    - See enclosed message schedule with signage listed by location, sign type, verbiage, description, and comments, if any.

END OF SECTION